**HTM63 COMPLIANT BASE AND WALL.**

* Manufacturer: David Bailey furniture

Tel: 01843 604896 [www.davidbaileyfurniture.co.uk](http://www.davidbaileyfurniture.co.uk)

* Standard: HTM 63
* Timber: To BS EN 942.

- Species: white melamine MDF 18mm.

* Appearance class: Not applicable.
* Moisture content on delivery: 9 to 13%.
* Finishes: As manufactured.
* Adhesive: To Manufactures Recommendations.
* Fixings: To Manufactures Recommendations.
* Fasteners: To Manufactures Recommendations.
* Joinery workmanship: As section Z10.
* Metalwork materials and workmanship: As section Z11.
* Other requirements:

Base Unit Carcases:

Plinth mounted: All plinths to be moisture resistant 18mm MDF

Construction: 18mm thick 750KG/m3 MDF fully assembled, internally dowelled and

glued and finished in white melamine MDF 18mm thick, 450mm deep. All base units to have 12mm white MDF backs.

Backs removable from within cupboard interior, for base units containing sinks or plumbing. In order to access service void behind cupboard (usually 150mm deep service void where 650mm deep work surface are used).

Door and Drawer Fronts:

Construction: Standard range laminate on 18mm MDF core complete with 2mm

thick PVC lipping.

* Drawer boxes:

Construction: Metabox metal sided drawer construction on standard metal runners with 12mm thick melamine MDF base and 18mm melamine faced MDF back. Drawer runners to be powder coated metal and support the underside of the drawer edge for maximum support. Nylon rollers. 3/4 and full extension drawer runners.

* Hinges: External 270° opening.
* Locks:

General security: Symo 3000 cylinder lock. Where requested.

* Drawer unit locks: Separate locks supplied to each drawer.
* Stainless steel D handles.

**CLINICAL WORKTOPS.**

* Manufacturer: David Bailey Furniture

Tel: 01843 604896 [www.davidbaileyfurniture.co.uk](http://www.davidbaileyfurniture.co.uk)

* Standard: HTM 63

Worksurfaces:

Depths vary from 300mm to 1000mm.

Standard heights: Standing height = 900H, Sitting ht = 740H

* Profile: 40mm – 55mm thick bullnose at front plus 50mm high integral rear upstand, giving 90mm overall worktop height.

Finishes: Postforming grade laminate on 18-36mm MDF core.

**SHELVING SYSTEM FOR GENERAL USE**

* Manufacturer: David Bailey Furniture

Tel: 01843 604896 [www.davidbaileyfurniture.co.uk](http://www.davidbaileyfurniture.co.uk)

* 1. Product reference: Spur shelving system.
* Shelves:
* Material: White melamine faced chipboard/MDF with high impact PVC edging to all exposed edges.
* Finish/ Colour: White.

Other components: uprights and support brackets.

**SHELVING SYSTEM**

* Manufacturer: David Bailey Furniture

Tel: 01843 604896 [www.davidbaileyfurniture.co.uk](http://www.davidbaileyfurniture.co.uk)

* 1. Product reference: Spur shelving system.
* Shelves:
* Material: Laminate faced MDF with high impact PVC edging to all exposed edges.
* Finish/ Colour: tba
* Other components: Spur Uprights and support brackets.

**HTM71 BASE AND WALL CUPBOARDS**

Drawing Ref : Ref to Schedules for size and type

Manufacturer: supplied by:

David Bailey Furniture. Tel: 01843 604896

[www.davidbaileyfurniture.co.uk](http://www.davidbaileyfurniture.co.uk)

Product: HTM71

* + ALL units within clinical areas to be made to the specification outlined below so they meet HTM71 standards.
	+ Doors & drawer fronts to be:-

High pressure laminate faced MFC core with high impact PVC edging to all exposed edges and assembled using steel mechanical fixings.

* + Plinths:-

Constructed from 18mm black melamine faced moisture resistant MDF.

* Hinges to be:- Exposed knuckle 270 °

2No Hinges for doors up to760mm high.

4No Hinges for doors up to 2000mm high.

* + Handles to be:-

Stainless steel SAA D-handles = 10mm dia. x 96mm long

* + Telescopic runners and support frames to be:-

Runner = Zinc plated steel 100% extension slides.

Frame = 'Rilsan' fine powder coated steel.

* + Base/wall unit trays manufactured in Polycarbonate. To the following dimensions:

600mm x 400mm x 50mm

600mm x 400mm x 100mm

600mm x 400mm x 200mm

-Or 455 wall/ reduced depth tall units

400mm x 300mm x 50mm

400mm x 300mm x 100mm

400mm x 300mm x 200mm

* + Locks:-

Standard Cupboards - Symo 3000. Where requested.

**STANDARD BASE AND WALL UNITS**

* Manufacturer: David Bailey Furniture

Tel: 01843 604896 [www.davidbaileyfurniture.co.uk](http://www.davidbaileyfurniture.co.uk)

* 1. Product reference: Healthline range.
* Finishes: As manufactured.
* Adhesive: To Manufactures Recommendations.
* Fixings: To Manufactures Recommendations.
* Fasteners: To Manufactures Recommendations.
* Joinery workmanship: As section Z10.
* Metalwork materials and workmanship: As section Z11.
* Other requirements:

Base Unit Carcases:

Construction: 18mm thick 750KG/m3 MDF fully assembled, internally dowelled, glued and finished in white melamine MDF 18mm thick, 565mm deep. All base units to have 12mm white MDF backs.

Plinth mounted: All plinths to be moisture resistant 18mm MDF

Backs removable from within cupboard interior, for base units containing sinks or plumbing. In order to access service void behind cupboard (usually 150mm deep service void where 650mm deep work surface are used).

* Doors & drawer fronts to be:-

 High pressure laminate faced MFC core with high impact PVC edging to

 all exposed edges and assembled using steel mechanical fixings.

* Hinges to be:- Exposed knuckle 270 °

 2No Hinges for doors up to760mm high.

 4No Hinges for doors up to 2000mm high.

* Handles to be:-

 Stainless steel SAA D-handles = 10mm dia. x 96mm long